## Slide 1: kagome data

## Slide 2: Content
Previous studies
The results of t/J=3 t2/t=0.7
  Electron density
  Superconductivity correlation
The results of t/J=0.5 1 2 5 7 10
The results of t2/t = - ( 0.1 — 0.7 )
The results of t/J=3
  t2/t=0 J2=- ( 0.1 — 0.7 )
  t2/t=0.3 J2=- ( 0.0 — 0.7 )
  t2/t=0.3 J2=- ( 0.0 — 0.7 )

## Slide 3
Doping quantum spin liquids on the Kagome lattice
March 2021. Cheng Peng, Yi-Fan Jiang
Content
  We review recent density-matrix renormalization group (DMRG) studies of lightly doped quantum spin liquids (QSLs) on the kagome lattice
Section II Doping gapped spin liquid
  lightly doped QSL of the AFM Heisenberg model on the kagome in the context of the t-J model
  Results by introducing additional second-neighbor electron hopping terms
Section III Doping critical spin liquid
  lightly doped critical spin liquid of the AFM XY model on the kagome lattice
Section IV Doping chiral spin liquid
Result
  While a number of distinct conducting phases, including high temperature superconductivity, have been theoretically anticipated we find instead a tendency toward fractionalized insulating charge-density-wave (CDW) states.
  While the superconducting correlations are short-ranged, they can be significantly enhanced by second-neighbor electron hopping

## Slide 5
I Doping gapped spin liquid ~ spin-spin correlation functions
Remarkably insensitive to doping concentration δ
Independent of YC6/YC8
F(r) decays exponentially at long distances and can be well fitted by an exponential function F(r) ∼ e−r/ξs with short correlation lengths ξs=1∼ 2 lattice spacings

## Slide 6
I Doping gapped spin liquid ~ superconducting correlations
All the SC correlations Φαβ(r) decay exponentially at long distances for both YC-6 and YC-8 cylinders and can be well fitted by the exponential function Φ(r) ∼e-r/ξsc
The SC correlation lengths ξsc = 0.5 ∼ 1.3 are small for all doping concentrations 0 < δ ≤ 11%

## Slide 7
I Doping gapped spin liquid ~ charge density (hole)
A clear CDW ordering is observed, although its pattern, i.e., unidirectional stripe or 2D crystal, depends on either the lattice geometry and doping concentration
The number of emergent unit cells is equal to the number of doped holes at all doping concentrations, showing that there are no Cooper pairs
Acdw remains finite in the Lx = ∞ limit (0.009 – 0.025)
Long-range CDW order

## Slide 8
I Doping gapped spin liquid ~ effect of second-neighbor hopping t'
The value of Φ(r) can be enhanced by many orders of magnitudes when t' is comparable with J and even more for larger t' (t=3, J=1)
The SC correlation length becomes significantly longer with the increase of t'
Quasi-long-range superconductivity has not yet been realized on the Kagome lattice
The oscillation amplitude Acdw of nh(x) becomes significantly smaller as t' increases

## Slide 9
For all these cases, we find that F(r) decays exponentially at long distances and can be well fitted by an exponentially falling function F(r) ∼ e-r/ξs
Although ξs slightly depends on δ and lattice geometry, it remains finite and small, e.g., ξs = 1.45(3)–2.1(2) lattice spacings for YC-6 and YC-8 cylinders.
There is no (quasi-) long-range magnetic order in the lightly doped critical spin liquid on the Kagome lattice
II Doping critical spin liquid ~ spin-spin correlation functions

## Slide 10
II Doping critical spin liquid ~ superconducting correlations
All types of the SC correlations decay exponentially at long distances for both YC-6 and YC-8 cylinders
The SC pair-pair correlations Φaa(r) for three different doping concentrations can be well fitted by an exponential function Φ(r) ∼ e-r/ξsc with short SC correlation length ξsc = 0.62(2)–0.82(1) lattice spacings
There is no (quasi-) long-range superconductivity in lightly doped critical spin liquid phase on the Kagome lattice

## Slide 11
II Doping critical spin liquid ~ charge density (hole)
There is charge stripe (i.e., unidirectional CDW order) at low doping level, e.g., δ = 1/18 for YC-6 cylinders. For higher doping concentrations on YC-6 cylinders and lightly doped cases for both YC-8 and YC-10 cylinders, the CDW order is 2D
The number of the emergent unit cells is equal to the number of doped holes for all doping concentrations, which demonstrates the absence of Cooper pairs in this lightly doped critical spin liquid on the Kagome lattice

## Slide 12
II Doping critical spin liquid ~ charge density (hole)
The presence of long-range CDW order is directly evidenced by the observed finite amplitude Acdw in the long-cylinder limit Lx = ∞
The ground state of lightly doped critical spin liquid can also be considered as a CDW of spinless holons with spin charge separation, which is evidenced by the short-range spin-spin correlations and the absence of doping induced magnetic order

## Slide 13
III Doping chiral spin liquid ~ spin-spin correlation functions and superconducting correlations
At half-filling, Eq reduces to the J-Jχ model, which has a stable gapped CSL in a larger parameter region
For both YC-6 and YC-8 cases, the extracted SC correlation lengths are ξsc ∼ 0.8 unit cell, nearly independent on bond types αβ.
F(r) can be fitted by the exponential function F(r) ∼ e-r/ξs with a short correlation length ξs ∼ 1.3 and ξs ∼ 1.1 unit cell for YC-6 and YC-8 cases, respectively
J = 1 t = 3 Jχ=0.5

## Slide 14
While it is not very straightforward to establish the absence of hole pairs for 1/12 doping concentration in Fig.8(c), it is clear that for YC-6 cylinders with δ = 1/24 and 1/18 doping concentration as shown in Fig.8(a-b), the number of emergent unit cells is equal to the number of doped holes
Similar charge stripes with one doped hole are observed in the bulk of the YC-8 cylinder with δ = 1/24 doping concentration (Fig.8(d)), indicating that the charge stripes emerged from the doped CSL is robust as the systems become wider
nh(x) has a strong spatial oscillation whose amplitude barely decays or even increases from the boundary to the bulk of the system. Therefore, while we cannot perform the finite-size extrapolation, it is very likely that such a stripe CDW order appears to be long-ranged in the Lx = ∞ limit for YC-6 and YC-8 cylinders
Moreover, there is no doping induced magnetic order, from which we could conclude that the ground state of the system forms a stripe crystal of spinless holons with spin-charge separation.
III Doping chiral spin liquid ~ charge density (hole)

## Slide 15
electron density (t1=3 J1=1 t2/t1=0.7 J2/J1=0.49)

## Slide 16
(includes both A and B sites)

## Slide 21
掺杂1/12，1/9时，y方向平移对称性破缺

## Slide 22
superconductivity correlation（a-a bond）

## Slide 23
超导关联量级在10-3到10-7之间，相比于原始t-J模型来说，衰减变慢

## Slide 26
electron density : YC-6，Lx=16，doping=1/18，2000state，14sweep，rb37
t=0.5/1时，系统都具有y方向平移对称性，电子分布与t=3有差异(t变小时边界电子密度下降)，但CDW的周期都是4，振幅也都是0.01左右

## Slide 28
t=2/3/5时，系统都具有y方向平移对称性，电子分布非常相似

## Slide 30
t=7/10时，系统都具有y方向平移对称性，电子分布与t=3有差异(t变大时边界电子密度上升)，但CDW的周期都是4，振幅也都是0.01左右

## Slide 32
superconductivity correlation
如果t=0时，变回自旋J1-J2模型，超导关联仍然如此吗？

## Slide 33
ab bond
aa bond
t=5
bb bond
ba bond
cb bond
cc bond

## Slide 38
判断：
存在CDW，满足y方向平移对称，但CDW振幅变强很多，可能意味着抑制超导

## Slide 39
t=3 t2/t=0.7
判断：超导关联相对于t2/t>0大幅下降，decay速度提高了约5个量级

## Slide 40
t=3 J=1 YC-6 Lx=16 δ=1/18

## Slide 45
判断：
随着引入J2，总体来说CDW被抑制了
基本满足y方向平移对称性

## Slide 46
判断：超导关联衰减仍比较快，结果不如t2/t=0.7,J2=049

## Slide 47
没有J2的时候，CDW振幅类似，超导关联函数的量级基本相同
加负的J2后，超导关联函数变弱

## Slide 53
判断：t2/t=0.3 J2<0时，结果都基本满足y方向上平移对称性。电子分布出现了很奇怪的鼓包

## Slide 55
判断：加负的J2后，超导关联函数出现了不规则的衰减，但总体变弱

## Slide 60
判断：t2/t=0.7,J2<0时，y方向基本满足平移对称性。电子密度出现了类似的鼓包，但是振荡更加剧烈

## Slide 63
2000states
3000states

## Slide 64
2000states
3000states

## Slide 65
判断：计算结果的奇异特征应该不是计算精度不够导致，计算是基本可靠的